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Tender Specification:		EXPANDED METAL
Application:				Facade, cladding, staircase railings,…etc. 

Expanded metal e,g. mesh type “ProMetall - LEOBERSDORF“, 

Material quality VARIANT A)
Aluminium raw
Material thickness 2 mm; total thickness approx. 21 mm; weight approx.4.2 kg/m²
light diameter at frontal view approx. 30 %, 
expanded material production in accordance with DIN791; standard tolerances
to define: 
· Assembly direction: long diagonal of the mesh (LD) HORIZONTAL or VERTICAL 
· View outside = “NOSE SIDE! or “FLAT SIDE” of the expanded metal
· Mesh direction / openings DOWNWARDS (“nostrils“ downwards) or UPWARDS
· Cut / mesh: CLOSED mesh horizontal/vertical
or OPEN mesh (recommended with edging in angular frame only)
· Installation type / visual effect: JOINT-TO-JOINT installation closed mesh horizontal and vertical with visible installation joints or CONTINUOUS MESH LOOK with tailored mesh and barely visible installation joint
· Installation type / technique: RIVETING of the expanded metal by means of stainless steel rivets directly with UK or WELDING of the expanded metal in angular frame + BOLTING TOGETHER with UK by means of mounting holes 

Formats in accordance with separate drawings / or fixed formats according to the below list:
LD xy  x   z   mm
LD xy  x   z   mm
Tolerances to be agreed in accordance with order.

Option / surcharge for surface processing:
a) Anodising on both sides anodised colour: standard colourless E6/C0
b) Anodising on both sides anodised colour: special according to the principal’s choice
c) [bookmark: _Hlk112206578]Powder-coating on both sides in accordance with RAL-standard
d) Powder-coating on both sides special colour according to the principal’s choice

Supplier: ProMetall www.prometall-europe.com / sales@prometall-europe.com or equivalent

Material quality VARIANT B)
Steel raw, subsequently hot-dip galvanised in accordance with DIN EN ISO 1461
Material thickness 1.5 mm; total thickness approx. 21 mm; weight not galvanised approx. 9.3 kg/m²

Option / surcharge for surface processing:
a) Powder-coating on both sides in accordance with RAL-Standard
b) Powder-coating on both sides special colour according to the principal’s choice

Material quality VARIANT C)
Special material to be defined (e.g. copper, bronze, brass, zinc…)
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